## Slide 1: Cryogenic systems for a PrFeB-based cryogenic permanent magnet undulator at TPS
Jui-Che Huang1, Hideo Kitamura2, Chin-Kang Yang1, Chih-Sheng Yang1, Cheng-Hsing Chang1, Cheng-Hsiang Chang1, Ching-Shiang Hwang1
1National Synchrotron Radiation Research Center, Taiwan
2RIKEN/SPring-8,Japan
ICEC27-ICMC 2018, Oxford, U.K.

## Slide 2: Undulators
The undulator is designed as a X-ray source from a third-generation light facility. Main features of an optimized source are;
Most important is the generation of a high magnetic field in a short period undulator.
-- the quality of the electron beam. For example, a low emittance storage ring.
-- undulator radiation from short period undulators with low phase errors:
  shorter wavelength radiation.  Hard X-ray
  more periods for a given length.  Higher Brilliance
  low degradation of SR.  Higher Harmonics can be reached
First Cryogenic Permanent Magnet Undulator (CPMU) prototype SPring8 ,2004
First In-vacuum Undulator SPring8, 1993
SuperConducting Undulator (SCU) LURE, 1980
First permanent magnet undulator at SSRL-SLAC,1980

## Slide 3: SuperConducting Undulator
SCU0 at APS with a period length of 16 mm and 20.5 periods generating a magnetic field of 0.8T at a magnetic / vacuum gap of 9.5 mm / 7.2 mm.
SCU15 at KARA with a period length of 15 mm, 100.5 periods and a magnetic field of 0.73T at a magnetic/vacuum gap of 8 mm / 7 mm.
2x Sumitomo RDK415D
2x Sumitomo RDK408D2
Liquid Helium indirect cooling
APS (USA)
KARA(Germany)

## Slide 4: Cryogenic Permanent Magnet Undulator

## Slide 5: SCU or CPMU at TPS
SCU15 @ gap 8 mm  0.73T
Heatload > 5.3W
CPMU15 @ gap 4 mm1.31T
Heatload > 25 W
Several considerations: Magnetic field, Beam-induced heat load, cooling technologies, field measurement, cost …. TPS decided to adopt CPMUs as Phase-II insertion devices.
The calculation is based on TPS parameters, EGeV = 3 GeV, Ib = 500 mA, number of bunches = 600, bunch length = 4.65 mm (15.5 psec), circumference = 518 m, bending radius = 8.353 m and a distance of 5 m from the dipole magnet end to the undulator entrance.

## Slide 6: Development of the TPS CU15
Main desired features for the CU15 are low-phase-errors and high thermal stability against various heat loads.
Items | Unit | Values
Magnet structure |  | Hybrid
Magnet material |  | Pr2Fe14B (NMX-68CU)
Remanence ( Br ) | T | 1.40 at 293 K 1.67 at 77 K
Coercivity ( Hcj ) | kA/m | 1689 at 295 K 6200 at 77 K
Magnet size (x,y,z) | mm3 | 2.25 × 56 × 20
Pole material |  | Vanadium Permendur
Pole size (x,y,z) | mm3 | 3 × 46 × 16
Period | mm | 15
Min. magnetic gap ,Gmag | mm | 4
Min. vacuum gap , Gvac | mm | 3.8
Effective magnetic field | T | 1.30
Deflection parameter |  | 1.81
Number of periods |  | 133
Magnetic force | kN | 31.8
Total length | m | 2
Total cooler capacity | watts | 400 at 80K
Operating temperature | K | ~80

## Slide 7: Cooling system for CPMUs
Indirect cooling of PMs with LN2 with temperature control
Indirect cooling of PMs with cold head and temperature control
Direct cooling of PMs with LN2 without temperature control
SOLEIL HZB
IHEP
ESRF SLS
Diamond LS
NSRRC
SPring-8
LN2 cooling
Stable closed-loop LN2 cooling in operation. (cooling system is used for Monochromator/ Thermosiphon cooling system)
Cryo-cooler cooling
Cryo-cooler cooling can provide a wide range of PM temperature below 77K and obtain good magnetic performance for a PrFeB / (NdPr)FeB CPMU.

## Slide 8: Cryo-cooler
A cryo-cooler can provide a cooling power of up to ~200 watts at 80K. Two cold-heads are necessary for a two-meter CPMU.
Advantages :
Low initial investment for the cooling system.
Suitable for a facility without LN2 supply.
Neither welding nor pipe connections can cause a vacuum risk. Compatibility with storage ring ultra-high vacuum regulation.
Wide cooling margin, so the design of a cooling system is relative easy compared to a LN2 cooling system.
Disadvantages :
Operating costs are high.
Annual maintenance of cryo-coolers.
Must use a low vibration type cryo-cooler.
Advanced Research Systems DE110
Sumitomo CH110
Leybold 250MD
SuzukiShokan RF90S

## Slide 9: Features of TPS CPMU
Cryo-coolers to compensate for diverse sources of heat loads
Two low vibration cryo-coolers (~200Wx2 @ 80K) are used.
The vacuum of the cold-heads is separated from the storage ring vacuum making the design compatible with UHV rules for storage rings and with easy maintenance .
In-vacuum girder is made of OFHC with high thermal conductivity and low thermal contraction compared to aluminum.
Annealed flexible thermal straps increase thermal conductance by a factor of 3.5.
A 320W (40Wx8) heater is used to balance the beam-induced heat load.
RTDs (PT100) are calibrated to minimize tolerances in temperature measurements.
Thermal budget and temperature control
Hollow bellows-link rods reduce conduction heat transfer by a factor of 7. The bulkhead design is to suppress the air circulation inside the hollow space of the rods,which prevents condensation on the surface.
HV
UHV

## Slide 10: TPS CPMU, CU15
Thermal conductor bar
Heaters
Flexible thermal straps
Separated and Insulated vacuum
for cold-heads
Inner structure
Overall structure
Cold-head
Connected to a storage ring

## Slide 11: Temperature Control System
A temperature control system is mandatory for a NdFeB-CPMU operating at 140~150K. But, temperature control is optional for a PrFeB-CPMU, the reason we use it is because:
We can obtain a reproducible energy spectrum under various beam conditions
Compensate any residual temperature gradient to minimize field errors.
Heaters are installed along the side of the magnet arrays with high speed PID temperature controllers .
An optimum PID parameters of the temperature control is important to minimize the temperature fluctuation of magnets.
Magnet [K] | 140 | 120 | 100 | 80 | 55
Cooling bar [K] | 111~122 | 103~108 | 82~89 | 68~73 | 51~54
Cold-head[K] | 60.9 / 61.3 | 56.0 / 57.9 | 52.7 / 53.1 | 49.6 / 50.3 | 44.7 / 45.9
Estimated Heater power [W] | ~100 | ~80 | ~60 | ~40 | 0
Temperature distribution of CU15 at various input of heater power

## Slide 12
Chart: NO Temperature control
| -1001.25 | -821.25 | -641.25 | -461.25 | -281.25 | -161.25 | -41.25 | 18.75 | 138.75 | 258.75 | 438.75 | 618.75 | 798.75 | 978.75
TOP | 76.1 | 76.53 | 76.25 | 76.21 | 76.49 | 76.16 | 76.57 | 77.01 | 76.69 | 77.29 | 76.6 | 76.9 | 76.49 | 76.94
Bottom | 77.8 | 77.62 | 77.92 | 77.49 | 77.32 | 77.54 | 77.56 | 77.62 | 77.24 | 77.57 | 77.23 | 77.48 | 77.74 | 77.21
The lowest achievable temperature of PMs is ~ 55 K in 48 hours.
(cold-head : 45 K, thermal conductor bar: 52 K)
If the temperature of PMs is controlled to ~ 80 K, the cold head is 50 K, thermal conductor bar is 70 K.
In magnet arrays, the temperature variation within  0.4 K with temperature control system. (PT100 is calibrated , the tolerance is within  0.1 K).
At ~ 80 K, the magnet gap is 0.99 mm wider.
Total shrinkage of a 2m-copper-magnet-array is 5.65 mm.
Chart: Z [mm]
| -1001.25 | -821.25 | -641.25 | -461.25 | -281.25 | -161.25 | -41.25 | 18.75 | 138.75 | 258.75 | 438.75 | 618.75 | 798.75 | 978.75
TOP | 77.4 | 77.71 | 77.54 | 77.48 | 77.7 | 77.38 | 77.72 | 78.02 | 77.73 | 78.22 | 77.52 | 77.71 | 77.35 | 77.72
BOTTOM | 78.02 | 77.8 | 78.11 | 77.71 | 77.58 | 77.82 | 77.87 | 77.93 | 77.62 | 77.69 | 77.63 | 77.92 | 78.14 | 77.59
Cooling performance

## Slide 13: Reduction of vibration of chambers
Using Gifford-McMahon cryo-coolers, instead of solvary cryo-coolers.
Using a flexible-straps-adapter between cold heads and thermal conductance feedthroughs.
Advantages
Avoid vibrations from cold-heads to inner structure of CPMUs.
No inner stress between cold-heads and thermal conductance feedthroughs .
Disadvantages
Reduced thermal conductance.
Increased thermal contact resistance due to many components.
A temperature rise on magnets
Original Design
New Design
Flexible-straps-adapter
5 cm
solvary cryo-coolers
G-M cryo-coolers

## Slide 14: Summary
  A 2m-CPMU has been tested at NSRRC with a vacuum compatibly in-situ measurement system.
  The PMs can reach 55K with two cold-heads (200W x2 @ 80 K). The heatload of TPS-2m-CPMU is estimated around 240 W.
  The temperature control can reduce the residual temperature gradient to a variation along the 2m-magnet-array to less than  0.4K.
  Using Gifford-McMahon cryo-cooler and flexible-straps-adapters can obtain lower vibration. But, the temperature of magnet may increase 5 K.
  Current design can be easily extended to LN2 cooling methods and the system is compatible with storage ring ultra-high vacuum regulations.
NdFeB

## Slide 15
Thank you very much.