## Slide 2: Heat transfer at dielectric – metallic interfaces in the ultra-low temperature range
J. Liberadzka1,2, J. Golm1, T. Koettig1, J. Bremer1, H.J.M. ter Brake2
1 CERN TE-CRG-CI, Switzerland
2 University of Twente, The Netherlands

## Slide 3: Content
Motivation – AEgIS experiment
Experimental setup
Cryolab DR characteristics
Steady state measurement results
  with magnetic field
  without magnetic field
Conclusions

## Slide 4: AEgIS at CERN
Antimatter Experiment:
Gravity, Interferometry, Spectroscopy
Picture: D. Krasnicky, AEgIS collaboration, presentation for LEAP 2018 Paris
Aim: direct measurement of the Earth’s gravitational acceleration g
on antihydrogen within 1 % precision

## Slide 5: AEgIS ultra–cold electrodes
Electrode requirements:
10 electrodes, some divided into 4 separate sectors,
Antimatter should „see” only golden surfaces,
Electrical insulation up to 1 kV,
Cooled below 100 mK
Compatible with ultra-high vacuum < 10-12 mbar,
Radiation hard
A. Kellerbauer, AEgIS collaboration,
Probing antimatter gravity – The AEgIS exeriment at CERN
Picture by G. Burghardt
24 mm
SAPPHIRE + GOLD

## Slide 6: Experimental setup – two types of sandwich
# 1
Optically polished 1mm thick sapphire disk
Stamp
Platform
125 μm indium foil
125 μm indium foil
520 nm Au
45 nm Ti
45 nm Ti
520 nm Au
# 2
+3 μm of vapour
deposited indium

## Slide 7: Experimental setup – preparation and measurements
Stamp
Sapphire disk with deposited thin layers
Platform
50 mm
Thermal resistivity:
A
MC
Clamping force can be removed!

## Slide 8: CERN Cryolab Dilution Refrigerator
Lowest recorded temperature 9.85 mK
Cooling power: 100 μW at 60 mK,
~500 μW at 90 mK
Mixing chamber of 120 mm diameter enables placing the samples in the mixture

## Slide 9: Steady state measurement results
Sapphire – In nc
Sapphire – Ti nc – Au
Magnetic field B=32.3 mT
↓
In and Ti nc
=
Thermal resistivity:
For single interface:

## Slide 10: The effective thermal resistivity depends on:
1. „Parallel plates effect” observed before by Peterson, Anderson (1972)
2. Phonon mean free path – estimation for sapphire below 1 K gives ~ 2 mm
4. Interface quality:
adhesion, ageing, alloying
3. Phonon wavelength

## Slide 11: Steady state measurement results
Sapphire – In sc - Cu
Sapphire – Ti sc – Au – In sc - Cu
Ti nc
No magnetic flux
↓
In and Ti sc
=
Including parallel
plates assumption
at the sapphire
disk:

## Slide 12: Conclusions
The „parallel plates effect” observed at the sapphire disk
Thin layers significantly reduce the effective thermal conductivity, even in normal conducting titanium
Only indium deposition at the bottom of the electrode
5 times better thermal performance!

## Slide 13
Thank you for your attention!