## Slide 2: Study of Thermal Diffusivity of Dielectric-Metal Interfaces at Low Temperatures
T. Koettig, P. Borges de Sousa, J. Golm, J. Liberadzka, J. Bremer
CERN, TE/CRG-CI Central Cryogenic Laboratory

## Slide 3: Content
Introduction to the test set-up
Method applied and samples
Measurements and numerical modelling
  - Copper as reference sample
  - Dielectric to metal interfaces
      Indium or titanium on sapphire
      SC cable via epoxy impregnation
Comparison: amplitude vs. - method
Conclusion

## Slide 4: Thermal conductivity / diffusivity set-up
Features:
3 temperature sensors calibrated to each other + offset compensation
Stepwise change of platform temperature 1 K - 2 K
ΔT on sample 0.2 K to 0.3 K
Passive thermal attenuator between cryocooler and thermal platform
Threshold frequencies (Stewart et al., Rev. Sci. Instrum. 54, 1 (1983):

## Slide 5: Measurement methodology I
λ - thermal conductivity
- heat load
L - length along x
A - cross section
- temperature difference
Thermal conductivity:
- thermal diffusivity
c - heat capacity
ρ - density
Amplitude method
Phase shift method
- thermal diffusivity in m2/s
L - length in m
µ - thermal diffusion length in m
Thermal diffusivity:

## Slide 6: Measurement methodology II
- method

## Slide 7: Diffusivity measurements on reference sample Cu-OFHC
Frequency dependence
At frequencies > threshold thermal diffusivity constant
Threshold frequency is higher at low temperatures
Oxygen-free high-conductivity
(OFHC) copper
Dimensions:
8 x 8 x 50 mm3

## Slide 8: Diffusivity measurements on reference sample Cu-OFHC
D(T) measured is in good agreement with literature values.
Amplitude method can be used for more complex samples
Samples and interfaces need to be adapted
Literature data from: J. E. Jensen et al., Thermal Diﬀusivity, Brookhaven National Laboratory Selected Cryogenic Data Notebook, Brookhaven National Laboratory (1980).
OFHC copper tested RRR~100 from th. conductivity results

## Slide 9: Thermal diffusivity of a Cu-In- sapphire and Cu-In-Au-Ti-sapphire sandwich
Indium sample : Cu-In-sapphire-In-Cu
Ti-Au sample: Cu-In-Au-Ti-sapphire-Ti-Au-In-Cu
See results presented by J. Liberadzka in her talk: E-09: 32
Definition of a diffusivity-like value (due to the presence of interfaces) =>
Link to
cryocooler

## Slide 10: Thermal diffusivity of a Cu-In-sapphire and Cu-In-Au-Ti-sapphire sandwich
Cu-In-Au-Ti-Sapphire
Influences by the cryocooler frequency and threshold frequency are visible
There is a clever solution to attenuate the cryocooler oscillations and increase
Cu-In-Sapphire

## Slide 11: Passive thermal attenuator (G. Dubuis)
Our version CERN Cryolab with:
Courtesy: G. Dubuis, X. He, and I. Božovic,
Sub-milliKelvin stabilization of a closed cycle cryocooler, Rev. Sci. Instrum. 85, 103902 (2014).
Attenuator
Pb and stainless steel disks +
Cu meander
No load temp. rises from 2.8 K to 3.4 K

## Slide 12: Thermal diffusivity of a Cu-In-sapphire and Cu-In-Au-Ti-sapphire sandwich
Measurement accuracy dT

## Slide 13: Thermal diffusivity of a Cu-In- sapphire and Cu-In-Au-Ti-sapphire sandwich
D*Cu-In-Sapphire > D*Cu-In-Au-Ti-Sapphire
D*max,Cu-In-Au-Ti-Sapphire is at lower T
Curves almost merge at about 3 K
Cu-In-Au-Ti-Sapphire has additional interfaces  additional thermal resistance
Numerical modelling of that structure =>

## Slide 14: Thermal diffusivity of a Cu-In-sapphire and Cu-In-Au-Ti-sapphire sandwich
Numerical modelling =>
measured thermal conductivity
Geometry +
Remaining deviation for Au-Ti-sapphire sandwich is attributed to the formation add. interlayers

## Slide 15: Comparing methods: amplitude attenuation vs. step function
Sample:
Nb3Sn Rutherford type cable stack of 11 T dipole, fully impregnated
a)
b)

## Slide 16: Conclusion
Evaluation of measurement methods
OFHC-copper measurement and comparison with literature values
Inhomogenous stackd with dielectric-metal interfaces
Comparison of methods for bulk samples
Amplitude attenuation and step methods seem to be complementary
CTD 101K

## Slide 18: Passive thermal attenuator
Courtesy: G. Dubuis, X. He, and I. Božovic,
Sub-milliKelvin stabilization of a closed cycle cryocooler, Rev. Sci. Instrum. 85, 103902 (2014).
Attenuator
Pb and stainless disks +
Cu meander

## Slide 19: HiLumi LHC11 T Nb3Sn Dipole => CTD-101K bulk epoxy sample
From: Frey, H. and Haefer, R. A., Tieftemperaturtechnologie

## Slide 20: Further diffusivity measurement methods
Pulse:
  is the distance between the heater and the sensor and
  is the time at which the temperature at reached its maximum value
Pulse 2:
  is the experimental temperature rise
  Plot ,
  diffusivity can be extracted through the slope of the resulting curve as
Step:
  plot as a function of
  is the time when reaches half of the maximum temperature rise
3 ω method and more …
Ref.: Hunklinger, S., Low Temperature Physics, Springer, 2005.
Ref.: Krüger, R. et al., Phys.
Stat. Sol. (a) 17: 471–478 (1973)
Ref.: Parker, W.J., Journal of
Applied Physics, 32, 1679-1684 (1961)

## Slide 21: l and k* of a Cu-In-sapphire and Cu-In-Au-Ti-sapphire sandwich
Indium (SC) Indium (NC)
Modelling of thermal conductivity including the boundary resistances e.g. Cu-In-sapphire:
Gmelin et al., J. Phys. D: Appl. Phys. 32 (1999) R19–R43.
Modelling of diffusivity including l measured !
of Cu-In-sapphire:

## Slide 22: l and k* of a Cu-In-sapphire and Cu-In-Au-Ti-sapphire sandwich
Cu-In-Au-Ti-sapphire = (2.7)
Geometry factor: static vs. transient
Remaining deviation for Au-Ti-sapphire sandwich is attributed to the formation add. interlayers
Modelling of thermal conductivity including the boundary resistances e.g. Cu-In-sapphire:
Gmelin et al., J. Phys. D: Appl. Phys. 32 (1999) R19–R43.