## Slide 1
Experimental and numerical study of the different quench acceleration phenomena in the JT-60SA Toroidal Field coils
Yawei HUANG¹, Walid ABDEL MAKSOUD¹, Bertrand BAUDOUY¹, Daniel CIAZYNSKI², Patrick DECOOL², Laurent GENINI¹, Benoît LACROIX², Sylvie NICOLLET², François NUNIO¹, Alexandre TORRE², Roser VALLCORBA¹, Louis ZANI²
¹CEA, IRFU, 91191 Gif-sur-Yvette Cedex, France
²CEA, IRFM, 13108 Saint-Paul-lez-Durance, France
E-mail: ywhuang90@gmail.com, yawei.huang@cea.fr

## Slide 2
Outline
Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
Experimental analysis of the different quench acceleration dynamics
  Quench resistance evolution
  Testing temperature conditions
Numerical analysis of the temperature oscillation effect on the quench acceleration
  Numerical model
  Oscillation amplitude
  Phase shift
Conclusions
Outline

## Slide 3
Context and introduction
Outline
Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
Experimental analysis of the different quench acceleration dynamics
  Quench resistance evolution
  Testing temperature conditions
Numerical analysis of the temperature oscillation effect on the quench acceleration
  Numerical model
  Oscillation amplitude
  Phase shift
Conclusions

## Slide 4
Why JT-60SA?
(Tokamak machine)
ITER “Broader Approach”:
  Superconducting Tokamak JT-60SA (Naka Japan) by Japan and Europe
  Operation experiences and key physics issues for ITER and DEMO reactors
Why quench test?
18 (+2 spare coils) superconducting Toroidal Field (TF) coils manufactured in France and in Italy, tested at CEA in France
  To check the coils performance and mitigate the fabrication risks
  To ensure the magnet security and Tokamak operations
I. Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol

## Slide 5
TF coil = casing + winding pack + insulation
Winding pack = 6 double-pancakes (DPs)
= 12 pancakes ()
Cable In Conduit Conductor (CICC):
  Cable section = 1/3 NbTi + 2/3 Cu
  Void fraction = 32% (Helium)
I. Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
7.5 m
4.5 m

## Slide 6
Instrumentation hydraulic
  Pressure
  Temperature
  Mass flow rate
Instrumentation electric
  Voltage: DP + joints + feeders
  Current
I. Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol

## Slide 7
Quench moment
0.05 K/min
0.4 K/min
Quench test protocol
1st step: nominal conditions
I. Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
2nd step: temperature-increasing phase

## Slide 8
Experimental analysis
Outline
Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
Experimental analysis of the different quench acceleration dynamics
  Quench resistance evolution
  Testing temperature conditions
Numerical analysis of the temperature oscillation effect on the quench acceleration
  Numerical model
  Oscillation amplitude
  Phase shift
Conclusions

## Slide 9
TFC10: “early” quench acceleration ~68%
 thermo-hydraulic quench-back [1,2]
TFC10bis: “delayed” quench acceleration ~26%  ???
Fast Discharge
2s delay
II. Experimental analysis
  Quench resistance evolution
  Testing temperature conditions
Quench resistance evolution of the side DP in the coil number 10
Acceleration:
[1] Huang Y, Abdel Maksoud W, et al 2017 Fusion Eng. Des. 124 147-152
[2] Lue J W and Dresner L 1994 Adv. Cryog. Eng. 39 437-444

## Slide 10
II. Experimental analysis
  Quench resistance evolution
  Testing temperature conditions
Before quench

## Slide 11
II. Experimental analysis
  Quench resistance evolution
  Testing temperature conditions
TFC10: “early” quench acceleration
TFC10bis: “delayed” quench acceleration
With

## Slide 12
II. Experimental analysis
  Quench resistance evolution
  Testing temperature conditions
Quench test TFC16
s
Quench test TFC10bis
s

## Slide 13
Numerical analysis
Outline
Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
Experimental analysis of the different quench acceleration dynamics
  Quench resistance evolution
  Testing temperature conditions
Numerical analysis of the temperature oscillation effect on the quench acceleration
  Numerical model
  Oscillation amplitude
  Phase shift
Conclusions

## Slide 14
Inter-turn thermal coupling model (in THEA)
  Heating flux terms
    Longitudinal thermal conduction
    Joule heat of the cable in case of quench
    Heat exchange by forced convection of supercritical helium flow
    External heat load per unit length on the insulation
    Transversal thermal conduction between conductors
  Thermal balance
  with
Ref: Y. Huang et al., “Numerical Modeling of the Quench Propagation
Phase in the JT-60SA TF Coils”, 2018 IEEE Trans. Appl. Supercond. 28 4204205.
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift

## Slide 15
Boundary conditions:
Inlet temperature with oscillation (in sinusoidal function):
Mass flow rate of helium per pancake ~2 g/s
Magnetic field map B(x) in the side DP
Friction factor f, forced flow convection coefficient
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift
0.05 K/min
0.4 K/min

## Slide 16
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift
Effect of oscillation amplitude on the quench acceleration dynamics (case of TFC16):
; ;
Case :
“delayed” quench acceleration
Case :
“early” quench acceleration

## Slide 17
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift
Temperature profiles at the quench initiation moment
Case (delayed):
  quench initiation at the coil’s inlet (x=0 m);
  higher
   lower
Case (early):
  quench initiation at the peak field region (x=2.5 m)
  lower
   higher
Conclusion: quench initiation location + temperature profile
 quench propagation
 normal zone length
(delayed)
(early)

## Slide 18
Special value of oscillation amplitude:
Why ?
Second parameter:
  Phase shift
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift

## Slide 19
III. Numerical analysis
  Numerical model
  Oscillation amplitude
  Phase shift
Effect of phase shift on the quench acceleration dynamics:
;
;
 Change the quench initiation position as well as the local between Tcs and helium (same reason to oscillation amplitude)

## Slide 20
Conclusions
Outline
Context and introduction
  Context of the project JT-60SA
  Characteristics of the Toroidal Field coil
  Quench test protocol
Experimental analysis of the different quench acceleration dynamics
  Quench resistance evolution
  Testing temperature conditions
Numerical analysis of the temperature oscillation effect on the quench acceleration
  Numerical model
  Oscillation amplitude
  Phase shift
Conclusions

## Slide 21
Issue: « delayed » quench acceleration phenomenon
Experimental analysis
  Observation : two quench tests in the same coil TFC10
          two different quench acceleration dynamics
  Assumption: effect of the testing temperature oscillations
Numerical analysis
  Single pancake model in THEA code
     Representative delayed case: TFC16
  Oscillation amplitude and phase shift: predominant effect on the quench acceleration dynamics.
    When the temperature oscillation is strong enough to initiate a quench far away from the peak field region and to lead to a globally high temperature difference between Tcs and helium, the “delayed" quench acceleration will be easier to take place. Otherwise, it will be an “early" one.
Conclusions

## Slide 22
THANK YOU