## Slide 1: Manufacture and Characterisation of Bulk MgB2 Superconductor with High Trapped Field for Biomedical Applications
Susie Speller
ICEC-ICMC, 4th September 2018, Oxford

## Slide 2: Acknowledgements
Oxford Materials (CfAS)
Sajjad Amirkhanlou
Guillaume Matthews
Tim Davies
Chris Grovenor
Element Six
Edwin Eardley
Chris Wort
Cambridge Engineering
John Durrell
Difan Zhou
David Cardwell
STFC (RAL)
Matthew Hills
Tom Bradshaw
Simeon Greenwood
Martin Crook

## Slide 3: Magnets for Biomedical Applications
Magnets for MRI body scanners are the main commercial application of superconductors.
Large expensive systems
Use NbTi superconducting electromagnets.
Cheaper limb-scale MRI machines are entering the market place.
Use 1 T permanent magnets.

## Slide 4: Magnetic Drug Targeting
Magnetic Force
Magnet
Blood vessel
Tissue
Drug
Magnetite
Polymer shell
Increasing magnetic force enables:
→ blood vessels deeper inside body to be targeted
→ effective trapping of drug carrier in larger diameter blood vessels with faster blood flow.

## Slide 5: Bulk superconductor magnets
To obtain high trapped fields:
→ large sample diameter
→ high critical current density
Challenges
Bulk superconductors need to be magnetised using an external magnetic field.
Cheap, compact, reliable cryogenic solutions are needed.
Demonstrators are needed to show these can be achieved in practical devices.
Advantages
Stronger than permanent ferromagnets (3-5 T for MgB2, 17 T for REBCO compared to ~1.6 T for Nd-Fe-B)
More compact than electromagnets

## Slide 6: Bulk MgB2 magnet demonstrator
3 year EPSRC grant to build a compact demonstrator magnet using bulk MgB2 superconductor
MgB2 bulk development (Dec 2017)
  Oxford
  Element Six
Cryogenics (Sep 2017)
  STFC
Pulsed field magnetisation (Sep 2018)
  Cambridge
OVC top hat
Main outer vacuum can
Neon pot
Radiation Shield
LN2 bath
JT Heat Exchanger
High Temp. HX
MgB2 puck
27K
For details of cryogenics – see poster E-15:065 on Thursday

## Slide 7: Advantages of MgB2
Cheap.
Polycrystalline – grain boundaries are good pinning sites.
Can be processed by scalable techniques.
Relatively high Tc of 39 K.
Larger magnetic fields than permanent magnets (3-5 T).
Effect of grain size on Jc
Mikheenko et al, SUST. 20 (2007) S264

## Slide 8: MgB2 Processing
In-situ processing
T <900 oC
Inherent porosity
Good grain connectivity
Ex-situ processing
T >900oC
High density (if processed under pressure)
Poor grain connectivity
Porosity
Poor sintering
Yamamoto et al 2012 Jpn. J. Appl. Phys. 51 010105
In-situ
Ex-situ

## Slide 9: Carbon doping
Carbon doping increases Jc at high fields - but reduces Tc.
Kim et al, NPG Asia Materials (2012) 4, e3
Lee et al, Physica C 397 (2003) 7

## Slide 10: Hot Pressing at Element Six
R&D presses at E6 GIC, Harwell UK
Industrial scale R & D presses at E6 Global Innovation Centre, Harwell.
High Pressure - High Temperature (HPHT) processing of large bulk samples under extreme conditions.
Temperature | 900-1500 oC (T1<T2<T3)
Pressure | 4-8 GPa
Time | 5-25 mins
Processing Conditions
Notes: High pressure: 55,000 atmospheres ( = tower of 5000 family-sized saloon cars stacked on a jar of peanut butter)

## Slide 11: Typical Microstructure
●
*
o
MgB2
MgB4
MgO
5 mm
BSE image
EDX phase map
MgB2
MgB4
MgO
MgB2
MgB4
MgO
X-ray Diffraction (XRD)
*
●
●
●
o
*
*

## Slide 12: Microstructural Refinement
5 mm
5 mm
5 mm
5 mm
Backscattered Electron Micrographs of Element Six HPHT for 15 mins.
Increasing Pressing Temperature
Increasing Grain Size

## Slide 13: Tc Measurements
T1 < T2 < T3
5 mT
Tc very close to optimum value of 39 K.

## Slide 14: Hysteresis Loops
All samples show hysteresis loops typical of polycrystalline type II superconductors with bulk pinning and well-connected grains.
Decreasing processing temperature increases size of hysteresis loop
20 K

## Slide 15: Jc(B) performance
At 20 K
At 27 K
T1<T2<T3
Lower processing temperatures → smaller grains → better Jc(B) performance

## Slide 16: Powder Modifications
Field-Assisted Sintering Technology (FAST)*
High energy Ball Milling
(BM)
50 MPa
* Guillon et al, Adv. Eng. Mat. 2014, 16, 830
Commercial MgB2 Powder
0.5-10 wt %
Y2O3 powder
additions
0-12 hours
5, 30 mins, 950-1150 oC

## Slide 17: Effect of Milling on Powders
MgB2
Y2O3
XRD of 2 wt% Y2O3 sample
Particle Size
Milling Time (h)
Median particle size (mm)
102
101
100
0
5
10
15
20
Counts
2q (o)

## Slide 18: XRD peak broadening analysis
As milling time increases:
→ lattice strain increases
→ crystallite size decreases

## Slide 19: Effect on Tc
Ball milling for 12 hours results in a small degradation in Tc.
Addition of Y2O3 results in two discernible transitions, with the first onset at a similar temperature to the sample made from as-received MgB2 powder.
Samples consolidated into bulks using FAST (1100 oC, 50 MPa, 5 mins)
Normalised Susceptibility
5 mT
35
36
37
38
39
40
41
Temperature (K)

## Slide 20: Effect on Jc
Samples consolidated into bulks (density >90%) using FAST (1100 oC, 50 MPa, 5 mins)
20 K
0
1
2
3
4
5
6
Jc (A/m2)
105
106
107
108
109
Applied magnetic field (T)
4 K
Applied magnetic field (T)
0
1
2
3
4
5
6
7
8
9
10
Jc (A/m2)
105
106
107
108
109

## Slide 21: Y2O3 Distribution
Y
O
Y
O
Y
O
BM 10 minutes
BM 1 hr
BM 12 hr
STEM EDX mapping of individual powder particles.
Increasing milling time results in finer scale mixing of Yttrium.
After milling for 12 hours, Y dispersed homogeneously within MgB2 particles.
2 wt % Y2O3

## Slide 22: Effect of Heat Treatment
2q (o)
MgB2 + 10 wt% Y2O3
XRD shows YB4 forms at the expense of MgB4 during sintering.
Higher processing temperature
→ increases YB4 fraction
→ restores crystallinity of MgB2

## Slide 23: Summary of Bulk Performance at 27 K
Jc (A/m2)
Applied Field (T)
FAST samples have highest Jc at low fields
Y2O3 additions make a small improvement in Jc(B)
Ultra HP synthesis at lower temperatures dramatically improves irreversibility field at 27 K.
Element Six HPHT sample
FAST samples

## Slide 24: Conclusions
Large diameter bulks have been made at E6 using HPHT process.
Ultra high pressure obtainable in E6 bulks allows densification at low temperature. The resulting small grain size leads to significant field enhancement at 27 K.
Initial work on Y2O3 additions have produced slight improvement in performance.
Future work includes more detailed microstructural studies, measuring trapped field performance, using the E6 HPHT process with our in-house modified powders, investigating other nanoparticle additions and scaling up to larger diameter bulks.

## Slide 25: Birr comparison
Birr (at Jc=106 A/m2) | 4 K | 20 K | 27 K
E6 (T1) HPHT | 9.5 T | 5.6 T | 3.1 T
0.5 wt% Y2O3 FAST | 7.5 T | 4.1 T | 2.3 T
As-received MgB2 FAST | 6.6 T | 3.8 T | 2.2 T

## Slide 26: E6 samples at 4.2 K