## Slide 1
M. Ranot1, Y. S. Oh1, S. H. Kang1, S. H. Jang2, D. Y. Hwang2, and K. C. Chung1
1Korea Institute of Materials Science, Changwon, Korea
2Kiswire Advanced Technology Ltd, Daejeon, Korea
Enhanced Jc at both self and high field of MgB2 superconductor
through co-doping route

## Slide 2
Carbon : Best dopant for MgB2
Solid-state mixing
Agglomeration of nano additives
Issue: homogeneous distribution
Nano additives are expensive
S. X. Dou et al., APL 81, 3419 (2002)
nano SiC-doped
S. Zhou et al., Adv. Mater. 19, 1373 (2007)
Sugar (C6H12O6)-doped
Wet-mixing process
Sugar coating of B powder
Reduction in self-field, Jc(H)
High MgO and high resistivity

## Slide 3
Solution process
C coating on B by pyrolysis of PMMA
Jc(H) and Jc(0). Little reduction in Tc
C-encapsulated Boron
RF plasma technique
Gaseous source of C
Good Jc(H) performance
J.H. Kim et al., Adv. Mater. 23, 4942 (2011)
Carbon : Best dopant for MgB2
Ranot et al., JALCOM 724 (2017) 507

## Slide 4
Motivation for this work
Wang et al., Phy. Rev. B 81, 224514 (2010)
Liquid doping source
Liquid SiCl4 free of Carbon
Better Jc, little reduction in Tc
Why Chloroform (CHCl3) ?
Liquid source
(i) easy for uniform mixing of powders
(ii) no solvent required
Can be coat on B at R.T.
Free of oxygen (O)
Cl and C co-doping effect
Molar mass of each element in CHCl3
M(Cl) = 89.095 %
M(C) = 10.061 %
M(H) = 0.844 %

## Slide 5
Preliminary study
(Mg + B) + CHCl3
Coating approach more favorable for Jc enhancement
as compared to addition approach.
Coating approach
Addition approach
Mg + (B + CHCl3)

## Slide 6
TEM for doped Boron
TEM for CHCl3 treated Boron
~6 nm
Amorphous
carbon
~3 nm
TEM, Elemental Mapping Analysis
Amorphous carbon layer formed on the surface of Boron powder
Chlorine element also found inside the Boron

## Slide 7
M-T curves of MgB2 with CHCl3
CHCl3 | Tc (K)
Pure | 37.50
0.5 ml | 37.74
1 ml | 37.65
2 ml | 36.79
4 ml | 35.84
8 ml | 35.35
12 ml | 34.75
No noticeable change in Tc with chloroform less than 1ml
Tc decreased when chloroform used more than 2 ml (Carbon substitution)

## Slide 8
XRD patterns of MgB2 with CHCl3
Shift in (100) and (110) reflections towards higher angles, no shift in (002)
a-axis
c-axis

## Slide 9
C & Cl element analysis of MgB2
Carbon content
(calculated, at. %)
Carbon content
(measured, wt. %)
CS Analyzer (CS744, LECO)
Both C and Cl amount was found to be increased
upon increasing the doping level of chloroform.
EDS analysis
Chlorine content
(measured, wt. %)
Calculated from XRD

## Slide 10
Jc(H) properties of MgB2
Systematic enhancement in Jc upon with the doping level of chloroform
Improvement of Jc both at low & high fields and 5 & 20 K

## Slide 11
Conclusions
Chloroform-doped MgB2 bulk samples were prepared
using coating approach.
TEM elemental mapping confirms the presence of C and Cl
on B powder.
Enhancement in Jc(H) was observed with CHCl3 doping
as compared to un-doped MgB2.
Enhancement could be attributed to the combined effect
of C and Cl.

## Slide 12
Acknowledgements
This work was supported by industrial Technology Innovation Program (Grant No. 10053590) funded by the Ministry of Trade, Industry and Energy (MOTIE), Korea
Thank you very much
for your kind attentions

## Slide 13
Jc-B property of MgB2 at 20 K
Jc at low-fields increased
up to 2 ml of CHCl3 possibly due to the only Cl doping(?)

## Slide 14
Flux pinning property
Doped samples showed much higher flux pinning force than that of un-doped MgB2.